50mm Down Aggregate

High Calcium Chalk - Calcium carbonate CaCO3

A high purity white calcium carbonate product which is made by crushing and screening chalk.

Typically used as graded trench-fill, capping aggregate or fill aggregate.

Typical		Specification

Chemical Analysis     (Dry Basis)				% Mass		% Mass

Calcium carbonate		CaCO3			96.5

Silica				SiO2			2.69

Magnesium oxide		MgO			0.24

Aluminium oxide		Al2O3			0.17

Ferric oxide			Fe2O3			0.13

Carbon			CO2			42.6

Sulphur			SO3			0.02

Free Moisture						6 - 10

Physical Analysis

- Passing %

Particle Size			50			100.0			100.0

25			68.1

3.35			17.9

Bulk Densities			kg/m3		 	1470

Los Angeles Abrasion - LA				37

Optimum Moisture					10%

All product specifications are based on tests carried out prior to despatch of product.

This specification relates to product numbers: 	355001						Last Revision Date: March 2018

Storage Recommended minimum bulk silo capacity for quicklime/Aqualime® 60m3, Ultralime® 120m3.

Further advice/information available on request.

Safety 	Refer to our Safety Data Sheet.