50mm Graded Aggregate

High Calcium Chalk - Calcium carbonate CaCO3

A high purity calcium carbonate product which is made by crushing and screening hard quarried chalk.

Typically used as a drainage aggregate, trench-fill, capping aggregate, fill aggregate or for acid neutralisation and in chemical processes.

Typical		Specification

Chemical Analysis* (Dry Basis)				% Mass		% Mass

Calcium carbonate		CaCO3			96.5

Silica				SiO2			2.69

Magnesium oxide		MgO			0.24

Aluminium oxide		Al2O3			0.17

Ferric oxide			Fe2O3			0.13

Carbon			CO2			42.6

Sulphur			SO3			0.02

Free Moisture						6 - 10

Physical Analysis

- Passing %

Particle Size			63			100.0			100.0

25			15.7

3.35			1.1			0-2.0

Bulk Densities			kg/m3			1400

*Chemical Analysis based on Woldlime Product  Data.

All product specifications are based on tests carried out prior to despatch of product.

This specification relates to product numbers: 	302001 - BULK				           Last Revision Date: March 2018

361001 - IBC

Storage Recommended minimum bulk silo capacity for quicklime/Aqualime® 60m3, Ultralime® 120m3.

Further advice/information available on request.

Safety 	Refer to our Safety Data Sheet.