6F5 Capping Aggregate

Selected Granular Material (Coarse Grading) - Imported onto Site

Definition - Unbound mixture complying with BS EN 13285. Any material or combination of materials - including recycled aggregates with not more than 50% by mass of recycled bituminous planings and granulated asphalt, but excluding materials that contain tar and tar-bitumen binders, unburnt colliery spoil, argillaceous rock and chalk.

| Conformity Requirements, Table 6/5 | Description | Requirement | Declared Value (Typical) |
| --- | --- | --- | --- |
| i | Size designation and overall grading category | As Below | As Below |
| ii | Maximum fines and oversize categories | As Below | As Below |
| iii | Los Angeles coefficient | <50 | 41 |
| iv | Volume stability of blast furnace slag | Not Applicable | Not Applicable |
| v | Volume stability of steel (BOF) and EAF) slag | Not Applicable | Not Applicable |
| vi | Other aggregate requirements | Not Applicable | Not Applicable |
| vii | Laboratory dry density and… | * | 2.201mg/m3 |
|  | Optimum water content | * | 10% |
| viii | Water content | Upper = Optimum wc Lower = Optimum wc - -2% | 9% |

| Grading Requirements, Table 6/5 | Requirement (%) | Declared Value (Typical) (%) |
| --- | --- | --- |
| 125mm | 100 | 100 |
| 80mm | 75-99 | 84 |
| 40mm | 50-99 | 75 |
| 20mm | 30-75 | 63 |
| 10mm | 15-60 | 19 |
| 2mm | 0-35 | 5 |
| 0.063mm | 0-12 | 2.6 |

All product specifications are based on tests carried out prior to despatch of product.

This specification relates to product numbers: 	354008					Last Revision Date: April 2016

Storage Further advice/information available on request.

Safety 	Refer to our Safety Data Sheet.