Aqualime® H20

Calcium Hydroxide Ca(OH)2/Water

Aqualime liquid lime is an aqueous suspension of calcium hydroxide (hydrated lime).

Typical		Specification

- Chemical Analysis     (As Received)			% Mass		% Mass

Calcium Hydroxide		Ca(OH)2		20

Water				H2O			80			75 - 85

- Chemical Analysis     (Dry Basis)

Calcium Carbonate		CaCO3			0.36

Silica				SiO2			0.19

Manganese Oxide		MnO2			0.01

Aluminium Oxide		Al2O3			0.04

Ferric Oxide			Fe2O3			0.02

Toxic Substances						mg/kg			mg/kg

Arsenic			As			0.3

Cadmium			Cd			0.3

Chromium			Cr			0.8

Mercury			Hg		        <	0.01

Nickel				Ni			3.1

Lead				Pb			0.8

Antimony			Sb		        <	0.01

Selenium			Se		        <	0.01

Physical Analysis

(Microns)		Passing %

Particle Size			75			100

Density			(g/ml)			1.13

Viscosity          Aqualime is a thixotropic suspension, for further information

please contact Singleton Birch

All product specifications are based on tests carried out prior to despatch of product.

This specification relates to product numbers: 	154501 - BULK					Last Revision Date: April 2016

154801 - IBC

Storage Recommended minimum bulk silo capacity for quicklime/Aqualime®  60m3, Ultralime® 120m3.

Further advice/information available on request.

Safety 	Refer to our Safety Data Sheet.