Aqualime® H35

Calcium Hydroxide Ca(OH)2/Water

Aqualime liquid lime is an aqueous suspension of calcium hydroxide (hydrated lime).

Typical		SpecificationkBl Chemical Analysis     (As Received)			% Mass		% Mass

BlankBlankBlankBlankBlankBlankBlankBlankBlankBlankBlankBlankBlankBlankBlankBlankBlankBlankBlank	Calcium hydroxide		Ca(OH)2		35

Water				H2O			65			60 - 65

- Chemical Analysis     (Dry Basis)

Calcium carbonate		CaCO3			0.40

Silica				SiO2			0.27

Manganese oxide		MnO2			0.01

Aluminium oxide		Al2O3			0.05

Ferric oxide			Fe2O3			0.02

Minimum Solids					35.0			35.0 min

Physical Analysis

(Microns)		Passing %

Particle Size			75			100

Density			(g/ml)			1.2

Viscosity          Aqualime is a thixotropic suspension, for further information

please contact Singleton Birch

All product specifications are based on tests carried out prior to despatch of product.

This specification relates to product numbers: 	153001 - BULK					Last Revision Date: April 2016

153501 - IBC

Storage Recommended minimum bulk silo capacity for quicklime/Aqualime®  60m3, Ultralime® 120m3.

Further advice/information available on request.

Safety 	Refer to our Safety Data Sheet.