Finelime® 2

High Calcium Quicklime - Calcium Oxide CaO

Finelime is a white calcium oxide powder which is made by crushing and screening quicklime.

Typical		Specification

Chemical Analysis     (Dry Basis)				% Mass		% Mass

Calcium oxide			CaO			94			90.0 min*

Silica				SiO2			1.9

Magnesium oxide		MgO			0.1

Aluminium oxide		Al2O3			0.23

Ferric oxide			Fe2O3			0.13

Carbon			CO2			3.4			6.0 max*

Sulphur			SO3			0.04

Physical Analysis

Reactivity 			Time (Mins)		Temp. C

0			20

2			55.7

5			67.8

Particle Size			Millimetres		Passing %		Passing Range %

5.00			100			95 - 100

3.35			100

1.00			76

Bulk Densities			kg/m3			990

*Specification based on in process testing of Burnt Lime 40 feedstock

All product specifications are based on tests carried out prior to despatch of product.

This specification relates to product numbers: 	124001 - BULK (MR)		Last Revision Date: April 2018

124501 - IBC (MR)

Storage Recommended minimum bulk silo capacity for quicklime/Aqualime®  60m3, Ultralime® 120m3.

Further advice/information available on request.

Safety 	Refer to our Safety Data Sheet.