Granulime® 5

High Calcium Quicklime - Calcium oxide CaO

Granulime is a white granular calcium oxide product which is made by crushing and screening quicklime.

Typical		Specification

Chemical Analysis     (Dry Basis)				% Mass		% Mass

Calcium oxide			CaO			93

Silica				SiO2			2.9

Magnesium oxide		MgO			0.42

Aluminium oxide		Al2O3			0.23

Ferric oxide			Fe2O3			0.13

Carbon			CO2			4.0

Sulphur			SO3			0.04

Physical Analysis

Particle Size			Millimetres		Passing %		Passing Range %

12.5			100.00

10			99.98

5			90.6

1			3.4

0.25			1.6

Bulk Density			kg/m3			775

All product specifications are based on tests carried out prior to despatch of product.

This specification relates to product numbers: 	120001 - BULK (MR)		Last Revision Date: March 2018

136001 - IBC1000

136501 - IBC500

Storage Recommended minimum bulk silo capacity for quicklime/Aqualime® 60m3, Ultralime® 120m3.

Further advice/information available on request.

Safety 	Refer to our Safety Data Sheet.