Microlime® 90

High Calcium Quicklime - Calcium Oxide CaO

Microlime is a fine, white calcium oxide powder which is made by pulverising and air classifying quicklime.

Typical		Specification

Chemical Analysis     (Dry Basis)				% Mass		% Mass

Calcium oxide			CaO			94			90.0 min*

Silica				SiO2			1.75

Magnesium oxide		MgO			0.42

Aluminium oxide		Al2O3			0.20

Ferric oxide			Fe2O3			0.14

Carbon			CO2			2.6			6.0 max*

Sulphur			SO3			0.03

Physical Analysis

Reactivity			Time (Mins)		Temp. C		Temp. Range C

0			20

2			64			47 - 75

5			71			58 - 78

10			70			62 - 79

Final			71			64 - 80

Particle Size			Microns		Passing %		Passing Range %

180			100

90			98			90 -100

45			83

Mean Particle Size		Microns		63

(Malvern d90)

Bulk Densities			kg/m3			900

*Specification Based on in Process testing of Burnt Lime 40 Feedstock.

All product specifications are based on tests carried out prior to despatch of product.

This specification relates to product numbers: 	112001 - Bulk		Last Revision Date: March 2018

116001 - IBC1000

116101 - IBC500

116501 - BAG25

116601 - BAG12.5

Storage Recommended minimum bulk silo capacity for quicklime/Aqualime® 60m3, Ultralime® 120m3.

Further advice/information available on request.

Safety 	Refer to our Safety Data Sheet.