Ultralime® Hydrated Lime

Calcium Hydroxide Ca(OH)2

Ultralime hydrated lime is a fine, white calcium hydroxide (hydrated lime) powder which is made by the reaction of quicklime with water.

Typical		Specification

Chemical Analysis (Dry Basis)				% Mass		% Mass

Calcium hydroxide		Ca(OH)2		96

Silica				SiO2			0.95

Magnesium oxide		MgO			0.09

Aluminium oxide		Al2O3			0.18

Ferric oxide			Fe2O3			0.12

Sulphur			SO3			0.04

Carbon			CO2			1.61

Free Moisture			H2O			0.7

BlankBlankBlankBlankBlankBlankBlankBlankBlankBlankBlankBlankBlankBlankBlankBlankBlankBlankBlklankBkBlankBlankBlankBlankBlankBlankBlankBlankBlankBlankBlankBlankBlankBlankBlankBlankBlank

Physical Analysis

Microns		Passing %		Passing Range %

Particle Size			600			100

200			99.9

90			98.6

Mean Particle Size		Microns		2-6

Specific Surface Area		m2/g			16-18.5

Bulk Density			kg/m3			400

All product specifications are based on tests carried out prior to despatch of product.

This specification relates to product numbers: 	140001 - BULK		Last Revision Date: March 2018

143001 - BAG25

144001 - IBC

Storage Recommended minimum bulk silo capacity for quicklime/Aqualime®  60m3, Ultralime® 120m3.

Further advice/information available on request.

Safety 	Refer to our Safety Data Sheet.