Woldlime

Screened chalk to comply with the Fertiliser Regulations 1991.

Agricultural Lime - Calcium carbonate CaCO3

A high purity white powder calcium carbonate product which is made by milling and screening chalk.

Typical		Specification

Chemical Analysis     (Dry Basis)				% Mass		% Mass

Neutralising Value					54

Calcium content as Ca	Ca			32

Calcium carbonate		CaCO3			96.5

Silica				SiO2			2.69

Magnesium oxide		MgO			0.24

Aluminium oxide		Al2O3			0.17

Ferric oxide			Fe2O3			0.13

Physical Analysis

- Passing %

Particle Size			45			100			98 min

25			100			97 min

6.3			98			98 min

2			50			30 min

Bulk Densities			t/m3			1.4

The above chemical and particle size analyses are carried out on a dry basis.

All product specifications are based on tests carried out prior to despatch of product.

This specification relates to product numbers: 	401001 - Bulk

401501 - IBC1000		Last Revision Date: March 2018

Safety 	Refer to our Safety Data Sheet.